# Specific Gravity of Soil Solids

- Introduction

Specific gravity, Gs, is defined as the ratio of the unit weight of a given material to the unit weight of water. The general ranges of the values of Gs are from 2.6 to 2.9. Table 1.1 gives the values of Gs for various soils. The method listed here is only applicable for soils that pass No. 4 U.S. sieve.

| Soil Type | Range of Gs |
| --- | --- |
| Sand | 2.63 – 2.67 |
| Silts | 2.65 – 2.7 |
| Clay and silty clay | 2.67 – 2.9 |
| Organic soil | < 2.0 |

Table 1.1: The ranges of Gs

- ASTM D-854

- Apparatus

- Volumetric flask: 500ml

- Thermometer

- Spatula

- Drying oven

- Evaporating dishes

- Sieve: No. 4 (4.75mm)

- Plastic squeeze bottle

Figure 1.1: Flask

- Aspirator: To remove entrapped air in water.

Figure 1.2: Aspirator

- Balance: The balance need to have a readability of 0.01 g and capacity of at least 2000 g.

Figure 1.3: Balance

- Actual Procedure

  - Clean the volumetric flasks and dry them.

  - Fill the flask No. 1 with water (tap water is accepted here) up to the 500 ml mark (bottom of the meniscus should be at the 500 ml mark).

  - Use a balance to determine the mass of the flask No. 1 (W1) with the water filled to the 500 ml mark.

  - Use the thermometer to determine the temperature of water in the flask No.1 (T1 oC)

  - Put 100 grams of air-dry soil that passes the No. 4 U.S. sieve into an evaporating dish.

  - If the soil is cohesive, mix the soil with water to the form of a smooth paste and let it soaked for about half to one hour. If the soil is granular, then skip this step.

  - Put the soil in to the volumetric flask No. 2.

  - Pour water into the volumetric flask No.2 to make it about two-third full.

  - Connect one end of the aspirator to the faucet and another end to the volumetric flask No. 2. Turn the faucet on. Then use the aspirator to remove the air entrapped in the water mixed with soil (Make sure that the entrapped air is removed thoroughly).

  - Make sure that the temperature of the water-soil mixture in the volumetric flask No. 2 is equal to the room temperature (T1 oC).

  - Pour more water into the volumetric flask No. 2 to the 500 ml mark.

  - Weigh the volumetric flask No. 2 with soil and water (W2).

  - Pour the content of the volumetric flask No. 2 completely into an evaporating dish. Make sure that there is no soil left in it (use the plastic squeeze bottle).

  - Use the oven to dry the soil.

  - Weigh the dry soil in the evaporating dish (Ws).

- Calculation and Formula

### Calculate the specific gravity, Gs:

Gs (at T1 oC) = Ws / Ww

Ws = the mass of the soil

Ww = (W1 + Ws) – W2, the mass of equal volume of water

### Specific gravity is usually reported at the temperature of 20 oC. So we need to convert the Gs (at T1 oC) to the Gs (at 20 oC).

Gs (at 20 oC) = Gs (at T1 oC) * A

The values of A are listed in the table 1.2

| Temperature (T1 oC) | A | Temperature (T1 oC) | A |
| --- | --- | --- | --- |
| 16 | 1.0007 | 24 | 0.9991 |
| 17 | 1.0006 | 25 | 0.9988 |
| 18 | 1.0004 | 26 | 0.9986 |
| 19 | 1.0002 | 27 | 0.9983 |
| 20 | 1.0000 | 28 | 0.9980 |
| 21 | 0.9998 | 29 | 0.9977 |
| 22 | 0.9996 | 30 | 0.9974 |
| 23 | 0.9993 |  |  |

Table 1.2 Values of A

- Sample Report

| Specific Gravity of Soil Solids |  |  |  |
| --- | --- | --- | --- |
| Description of soil |  | Specimen No. |  |
| Volume of flask at 20 oC ml | Temperature of solution oC |  |  |
| A (Table 1.2) |  |  |  |
| Location |  |  |  |
| Tested by |  | Date |  |
| Item |  | Test No. |  |
|  | 1 | 2 | 3 |
| Volumetric flask No. |  |  |  |
| Mass of flask + water filled to mark, W1 (g) |  |  |  |
| Mass of flask + soil + water filled to mark, W2 (g) |  |  |  |
| Mass of dry soil, Ws (g) |  |  |  |
| Mass of equal volume of water as the soil solids, Ww (g) = (W1+Ws) - W2 |  |  |  |
| Gs(T1 oC) = Ws / Ww |  |  |  |
| Gs(20 oC) = Gs(T1 oC) * A |  |  |  |
| Average Gs |  |  |  |