# V.b Falling Head

- Introduction

Water from a standpipe flows through the soil. Initial head difference h1 at time t = 0 is recorded, and water is allowed to flow through the soil specimen that the final head difference at time t = tF is h2.

- ASTM D-2434

- Apparatus

- Combination permeameter K-605A

- Thermometer

- Stop watch

- Rubber tubing

- Actual Procedure

- Slip the bottom porous stone into the specimen chamber.

- Collect oven-dry sand. Pour the sand into the specimen chamber in small layers, and compact it by vibration.

- After the specimen chamber is filled by sand about 2/3 full, slip the top porous stone into the chamber to rest firmly on the sand.

- Place a spring on the top porous stone.

- Close the cap and tighten the cap nuts.

- Measure the length (L) of the compacted specimen in the chamber.

- Supply water using a plastic tube from the water inlet to the burette. The water will flow from the burette to the specimen and then to the outlet on the chamber.

Figure 5b.1: Setup of Falling head permeability

- Remove the air bubbles in the tube.

- Allow the water to flow for some time in order to saturate the specimen.

- Close the outlet valve.

- Measure the head difference, h1, which is the vertical distance between the water level in the burette and the level of outlet.

- Open the valve. Water will flow through the burette to the specimen and then out of outlet. Record time (t) with a stop watch until the head difference is equal h2, which is the vertical distance between new water level and the level of outlet. Then close the valve.

- Determine the volume, V, of water that is drained from the burette in cm3.

- Add more water to the burette to make another run and change h1 and h2 all the time.

- Record the temperature, T (oC), of the water.

- Calculation and Formula

  - The coefficient of permeability k

L is the length of the specimen.

A is the cross-section of the specimen.

  - Temperature correction of k. The value k is usually given for a test temperature of water at 20 oC. The table 5a.1 shows the coefficient for different water temperature.

k (at 20oC) = k (at ToC) * Ck

| Temperature (ToC) | Ck | Temperature (ToC) | Ck | Temperature (ToC) | Ck |
| --- | --- | --- | --- | --- | --- |
| 16 | 1.106 | 21 | 0.976 | 26 | 0.869 |
| 17 | 1.077 | 22 | 0.953 | 27 | 0.850 |
| 18 | 1.051 | 23 | 0.931 | 28 | 0.832 |
| 19 | 1.025 | 24 | 0.910 | 29 | 0.814 |
| 20 | 1.000 | 25 | 0.889 | 30 | 0.797 |

Table 5b.1 Coefficient Ck

- Sample Report

| Falling Head Permeability Test |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Test No. | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 |
| L (cm) |  |  |  |  |  |  |  |  |  |
| A (cm2) |  |  |  |  |  |  |  |  |  |
| h1 (cm) |  |  |  |  |  |  |  |  |  |
| h2 (cm) |  |  |  |  |  |  |  |  |  |
| t (sec) |  |  |  |  |  |  |  |  |  |
| T(oC) |  |  |  |  |  |  |  |  |  |
| k (cm/s) |  |  |  |  |  |  |  |  |  |
| Average k |  |  |  |  |  |  |  |  |  |
| k at 20 oC |  |  |  |  |  |  |  |  |  |